Afbeelding met grijs, gebouw, beton, muur

Door AI gegenereerde inhoud is mogelijk onjuist.



**Product Description**

Type: Ceramic façade cladding, type: Classic - I-shaped

Textuur: unsanded, low texture

Color: Black Oxid

Black with brown-toned nuances

**Technical Properties**

* Dimensions (H x W x D approx.) 225x400x13 mm
* Pieces/m² approx. 12,5
* Dimensional tolerances

Width (in extruded direction): +/- 4 mm

Height (opposite to the extruded direction): +/- 2 mm

Thickness – according to EN ISO10545-2: 13 mm +/- 1 mm

Straighteness (in extruded direction) according to EN ISO 10545-2: +/- 1,5 mm

Orthoginality according to EN ISO 10545-2: +/- 2 mm

Flatness: +/- 2 mm

* Water absorption – according to EN ISO 10545-3 3-6%
* Weight: 2,5 kg/pcs +/- 0,5 kg
* Frost resistance – according to EN ISO 10545-12: frost resistant
* Reaction to Fire: Class A1
* Flexural strength - load (225x500 mm) – according to EN ISO 10545-4: > 750 N
* Resistance to thermal shock – according to EN ISO 10545-9: compliant
* Impact resistance – according to EN ISO 10545-5: 0,7-0,9
* Stain resistance – according to EN ISO 10545-14: group 5 (glazed)
* Chemical resistance – according to EN ISO 10545-13: group GA (glazed)
* Thermal expansion – according to EN ISO 10545-8: 5,75 x 10-6 K-1 +/-1

**Appearance Characteristics**

In a sample of 100 tiles, at least 95 shall be undamaged. Considered as damage: any broken tile, tiles with a broken corner or edge, or cracks in the applied layers, whether visible cracks (< 0.2 mm) or worn-off profiling, provided these are considered disturbing for the visible surface of the tile. The minimum diameter of a defect is 15 mm.

The number of defective tiles must not exceed 5 %. Considered as defects: the presence of inclusions that may cause flaking on the visible surface of the tile upon swelling, or cracks with a width ≥ 0.2 mm on the visible surface.

**Transport and storage**

Do not stack pallets during transport and storage to avoid breakage.

All data is provided by the manufacturer. Dimensions may vary depending on production. For the most up-to-date version, see [www.brickz.world](http://www.brickz.world). This document is not binding and supersedes all previous publications. The manufacturer reserves the right to modify the product range and its characteristics. The user must always ensure they have the most recent product description.